## Slide 1: EE 669 VLSI Technology Assignment 2: Solution of exercise questions
Kartik Chikkanagoudar
21D170023

## Slide 2: Lecture 7 Slide 14 : Exercise : sequence of process steps for replacement gate process
CMP and Gate Etching: A thick oxide layer is removed using chemical-mechanical polishing (CMP), and then the polysilicon gate is selectively etched away using a plasma etch process that stops on the gate oxide.
Gate Oxide Removal and Chemical Oxide Formation: The thin gate oxide is removed using a quick wet etch, revealing the bare silicon channel surface. To stabilize the interface between the silicon and the dielectric, a very thin (< 1nm) chemical oxide is formed on the silicon surface.
High-K Dielectric Deposition: A high-K dielectric material, such as hafnium oxide (HfO2), is deposited atomic layer by atomic layer in an ALD reactor. This process involves alternating between two precursors to build up the dielectric film one atomic layer at a time, resulting in a precise and controlled thickness of 2nm - 3nm.
Capping Layer Deposition: To protect the high-K dielectric from contamination and damage during subsequent processing steps, a thin capping layer of titanium nitride (TiN) is deposited using either ALD or sputtering.
Etch-Stop Layer Deposition: A thin tantalum nitride (TaN) layer is deposited to serve as an etch-stop layer. This layer allows for the formation of different metals in the NMOS and PMOS transistors, enabling control of the gate threshold voltage.
Metal Layer Deposition: A thick TiN layer is deposited everywhere to set the PMOS work function, while a deposited aluminum layer sets the work function for the NMOS device. Both gate stacks are then filled with a final metal, such as thick aluminum or tungsten.
CMP and Planarization: The entire surface is planarized using CMP to bring all the gate stacks to a uniform level, resulting in the final replacement metal gate (RMG) structure.
Low-Temperature Anneals: One or more low-temperature anneals (approximately 400°C) are performed during the stack depositions to induce some interdiffusion between the metal layers. This interdiffusion helps to correctly set the work function in the NMOS and PMOS devices, respectively.
Plummer and Griffin, Integrated Circuit Fabrication: Science and Technology, 2023
1

## Slide 3: Lecture 8 Slide 22 : Exercise 2 : Original vs Modern dual damascene process
Original Dual Damascene process | Modern Dual Damascene Process
SiO2 (PECVD)
SiO2 (PECVD)
Interlayer dielectric(SiO2)
Interlayer dielectric(SiO2)
SiO2 (PECVD)
SiO2 (PECVD)
Hard mask
Etch stop
Metal contact/layer
After second lithography
After second lithography
Before second lithography
Before second lithography
Plummer and Griffin, Integrated Circuit Fabrication: Science and Technology, 2023
2

## Slide 4: Lecture 8 Slide 22 : Exercise 2 : Original vs Modern dual damascene process
Original Dual Damascene process | Modern Dual Damascene Process
In the original process the first lithography would etch down to the lower etch stop layer. Hence a via would be formed across the two dielectric layers. After this the second lithography etches down to the middle etch stop in the pattern of the new metal layer and we get the etched metal layer pattern and via The problem with this process is that during second lithography the deep via created after first etch does not properly get cleaned of photoresist which causes issues in the deposition on metal in the via. Also since the surface is very non-uniform after first-etch the second lithography becomes more complex | In the modern process a hard mask is patterened according to the pattern of the new metal layer. Then in the first lithography the vias are etched down the middle etch stop. Hence we have a via in the first dielectric layer and a hard mask in the metal layer pattern on the top. The second dielectric layer is untouched. After this the second lithography etches the pattern of the hard mask down to the middle etch stop. Simultaneously the already etched via etched down to the lower etch stop forming the metal-contact via. This method proves to be better than the original since it provides a relatively flat surface for the second lithography
2nd dielectric layer
1st dielectric later
Interlayer dielectric(SiO2)
Interlayer dielectric(SiO2)
1st dielectric layer
2nd dielectric layer
Hard mask
Metal contact/layer
Plummer and Griffin, Integrated Circuit Fabrication: Science and Technology, 2023
3

## Slide 5: Lecture 8 Slide 23 : Exercise : create a sprocess input deck for simulating the process sequence to create a 180 nm gate length n-channel MOSFET
Plummer and Griffin, Integrated Circuit Fabrication: Science and Technology, 2023
1
The .cmd file for the sprocess input deck is submitted along with the this report, it can also be found in the google drive link given
below:
Gdrive link : sproc_21d170023.cmd
The following references were used in making the process file:
Sentaurus Process : Two dimensional process simulation
Sentaurus process manual